LASER BEAM MACHINING (LBM) (CUTTING/DRILLING/WELDING)

## (LASER İLE İŞLEME (KESME / DELME / KAYNAK))

LASER (Light Amplification Using Stimulated Emission of Radiation)

Sun's radiation:    7 kW/cm2  (on sun's surface)

In laser for short pulses:    10 kW/cm2 (on beam cross section)

# Principles

-If a laser beam is focused on (1/100) of mm2, E=105 kW/cm2, this heat vaporize any known materials.

-The laser rod is exited by xenon filled flash lamp, which surrounds it.

E(usable) = 106 - 107 kW/cm2

 = Eusable / Esupply = 0.5 - 50 %

# Material Removal Mechanism

Melting and evaporation of workpiece material under extensive heat.

## Utilization of heat energy

|  | - A part is reflected and lost. |
| --- | --- |
|  | - Most of energy is used for melting. |
|  | - Small part is for evaporation. |
|  | - Very small is conducted into unmelted base material. |
|  | - Very small is absorbed on the way and by the evaporated and emitted droplets. |

5-DOF Laser Drilling Machine

(a)

(b)

Figure 13.1 LBM Mechanism

# Laser Types and Materials

| Continuous waves (CW) |  | Heavy and continuous machining |
| --- | --- | --- |
| Pulsed waves |  | drilling of small areas |
|  |  | for thin material (sheets) |

Laser materials and performances

| Laser Material | Wavelength (m) | Mean Power (W) |  (%) | Relative Cost |
| --- | --- | --- | --- | --- |
| CO2 (gas) | 10.2 | 100 - 25.000 (400 - 1.500 common) | < 10 | 400 |
| Nd YAG (Continuous) * | 1.06 | Av. 400 (peak 20.000) | < 1 | 10 - 44 |
| Nd YAG (Pulsed) * |  |  |  |  |
| Argon (gas) | 351 - 529 | - | < 0.1 | 3 - 9 |
| CO (gas) | - | 2000 | 60 |  |

* Solid state of neodymium, yttrium-aluminum-garnet

# Metallurgical Effects

-Heat affected zone is very narrow (min. 0.025, max. 1 mm). For sheet materials, very little melting occurs and material is removed mainly by evaporation. No significant effect on metallurgical properties of work material.

-Heat affected zone is thinner than EDM.

Possibilities for Cutting (Figure 13.1a)

- Move the workpiece

- Move the laser equipment

- Move the lenses or mirror (the simplest way)

# Applications

## 1) LBM Drilling

-Round holes ranges from 0.127 - 1.27 mm can be drilled.

-L/D ratios = 100/1

-Heat affected zone thickness = 0.002 - 0.1 mm.

-Diametric repeatability = ± 0.025 mm (or 10% of the diameter)

Figure 13.2 Gas-assisted Laser Cutting

## 2) LBM Cutting (Figure 13.2)

-LBM Cutting = (Laser beam) + high velocity gas to melt, vaporize and oxidize (air, argon (used to prevent oxidation), oxygen (highest cutting speeds))

- Cutting of stainless steel is very wide.

-Holes with diameter larger than 10 mm or holes that are not round are produced by CNC contour cutting.

-Trepanning can be used to produce holes with diameter range 0.5 - 10 mm. L/D = 20/1 (Figure 13.3).

Laser trepanning                 Hole trepanning              Micro hole trepanning

Figure 13.3 Laser trepanning

Figure 13.4 LBM Cut Parts

Wood engraving   Wood engraving         Stamp engraving     Photo engraving

Cylinder items            Metal engraving               Plastic engraving

Figure 13.5 Laser Engraving

3) Laser Engraving (Figure 13.5): Laser engraving (or laser marking) is the practice of using lasers to engrave or mark an object. System is capable to engrave precisely on any metal and non-metal materials. YAG lasers (50-100W) and CO2 (80W/100W) are common. The engraving speed is 0-1000 mm/s. Worktables are electrical type with up and down movements.

## 4) LBM Welding: Used for spot and seam welding. Weld penetration is limited to a maximum of 2.5 mm.

# Advantages

|  | -No contact between workpiece and cutting tool |
| --- | --- |
|  | -Non-metallic materials can be machined (refractors, composites) |
|  | -Very thin layer of heat affected region |
|  | -Machining can be controlled by simply changing the direction of mirrors or lenses |
|  | -Very small diameters can be cut |
|  | -No harmful radiation |
|  | -Less skill of operators |
|  | -Easily adaptable for control systems |
|  | -Sharp corners can be cut by small spot of laser |
|  | -Laser head need not to be close proximity of workpiece (advantages for difficult accessibility cases). |
|  | -Can operate in any transparent environment like air, inert gas, liquids (some), KCl, germanium, diamond, glass, Zn Se, Cd Te. |

# Limitations

|  |  is low (high energy cost) |
| --- | --- |
|  | -High initial cost (18.000 - 100.000 $) |
|  | -Needs cooling of laser material |
|  | -Depth of cut is limited |
|  | -Laser beam reflects (some metals are difficult to cut, like Al (difficult), Cu) |
|  | -Hole walls are irregular and tapered |
|  | -Difficult to control hole diameter tolerance (at most ± 5% of hole diameter) |
|  | -Not applicable for blind machining |
|  | -Recast layer and heat affected zone |

| Video. Contour cutting Video. Pipe cutting Video. Stainless steel cutting (0.8mm) Video-High speed drilling (225holes/min) | Video. Thick steel cutting (20 mm thick) Video. Drilling - Cutting (2mm thick) Video. Steel sheet cutting (0.8 mm thick) |
| --- | --- |